# Urea

(Last updated April 2026)

Figure 1.  The molecular diagram of Urea.

# CSP studies

| REFCODE | UREAXX |
| --- | --- |
| Formula | C1 H4 N2 O1 |
| Common Name | Urea |
| IUPAC Systematic Name | Urea |
| Other Names |  |
| CSD Refcodes | UREAXX25, UREAXX26, UREAXX27 |
| Search Identifier | A |
| Scientist | Stephen Tendyra |
| Date | 2016 |
| Publication | With Matteo Salvalaglio |
| Energy model | 2 |
| Study_ID | 10 |
| Programs | Study_ID=20, CrystalOptimizer, DMACRYS (2.2.0.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\Urea\CrystOpt |
| Potential Description | CrystalOptimizer with GDMA2.2(PBE1PBE/aug-cc-pVTz) + FIT |
| Intramolecular Description | PBE1PBE aug-cc-pVTz |
| Energy model | 1 |
| Study_ID | 20 |
| Programs | Rigid CrystalPredictor, DMACRYS (2.2.0.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\Urea\CP_DMACRYS |
| Potential Description | GDMA2.2(PBE1PBE/aug-cc-pVTz) + FIT |
| Intramolecular Description | PBE0/aug-cc-pVTz |

Figure 2.  Crystal energy landscape of Urea from previous work.

# CSD structures (CSD version 6.01 with Feb 2026 update)

Table 1.  Crystallographic information for CSD entries for Urea.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| UREAXX | P-421m | 0.25 | 5.662 | 5.662 | 4.716 | 90.0 | 90.0 | 90.0 | 1.3192 | polymorph I |
| UREAXX01 | P-421m | 0.25 | 5.582 | 5.582 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3659 | polymorph I |
| UREAXX02 | P-421m | 0.25 | 5.589 | 5.589 | 4.6947 | 90.0 | 90.0 | 90.0 | 1.3600 | polymorph I |
| UREAXX04 | P-421m | 0.25 | 5.57600 | 5.57600 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3689 | polymorph I |
| UREAXX07 | P-421m | 0.25 | 5.57600 | 5.57600 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3689 | polymorph I |
| UREAXX08 | P-421m | 0.25 | 5.578 | 5.578 | 4.695 | 90.0 | 90.0 | 90.0 | 1.3653 | polymorph I |
| UREAXX09 | P-421m | 0.25 | 5.64500 | 5.64500 | 4.704 | 90.0 | 90.0 | 90.0 | 1.3305 | polymorph I |
| UREAXX10 | P-421m | 0.25 | 5.578 | 5.578 | 4.695 | 90.0 | 90.0 | 90.0 | 1.3653 | polymorph I |
| UREAXX11 | P-421m | 0.25 | 5.572 | 5.572 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3708 | polymorph I |
| UREAXX12 | P-421m | 0.25 | 5.565 | 5.565 | 4.684 | 90.0 | 90.0 | 90.0 | 1.3749 | polymorph I |
| UREAXX13 | P-421m | 0.25 | 5.57 | 5.57 | 4.688 | 90.0 | 90.0 | 90.0 | 1.3712 | polymorph I |
| UREAXX14 | P-421m | 0.25 | 5.58400 | 5.58400 | 4.689 | 90.0 | 90.0 | 90.0 | 1.3641 | polymorph I |
| UREAXX22 | P-421m | 0.25 | 5.66100 | 5.66100 | 4.712 | 90.0 | 90.0 | 90.0 | 1.3208 | polymorph I |
| UREAXX23 | P-421m | 0.25 | 5.6577 | 5.6577 | 4.7042 | 90.0 | 90.0 | 90.0 | 1.3245 | polymorph I |
| UREAXX24 | P-421m | 0.25 | 5.589 | 5.589 | 4.68 | 90.0 | 90.0 | 90.0 | 1.3643 | polymorph I |
| UREAXX25 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX26 | P21212 | 0.5 | 3.414 | 7.36 | 4.606 | 90.0 | 90.0 | 90.0 | 1.7233 | polymorph IV |
| UREAXX27 | P212121 | 1.0 | 3.539 | 8.234 | 8.79000 | 90.0 | 90.0 | 90.0 | 1.5573 | polymorph III |
| UREAXX28 | P212121 | 1.0 | 3.62350 | 8.272 | 8.844 | 90.0 | 90.0 | 90.0 | 1.5047 | polymorph III |
| UREAXX29 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX30 | P-421m | 0.25 | 5.638 | 5.638 | 4.714 | 90.0 | 90.0 | 90.0 | 1.3310 | Phase I polymorph |
| UREAXX31 | P-421m | 0.25 | 5.622 | 5.622 | 4.672 | 90.0 | 90.0 | 90.0 | 1.3506 | Phase I polymorph |
| UREAXX32 | P212121 | 1.0 | 3.62350 | 8.272 | 8.844 | 90.0 | 90.0 | 90.0 | 1.5047 | Phase III polymorph |
| UREAXX33 | P212121 | 1.0 | 3.589 | 8.252 | 8.833 | 90.0 | 90.0 | 90.0 | 1.5248 | Phase III polymorph |
| UREAXX34 | P212121 | 1.0 | 3.5299 | 8.236 | 8.785 | 90.0 | 90.0 | 90.0 | 1.5618 | Phase III polymorph |
| UREAXX35 | P212121 | 1.0 | 3.41700 | 8.162 | 8.87000 | 90.0 | 90.0 | 90.0 | 1.6124 | Phase III polymorph |
| UREAXX36 | P212121 | 1.0 | 3.4279 | 8.125 | 8.795 | 90.0 | 90.0 | 90.0 | 1.6284 | Phase III polymorph |
| UREAXX37 | P212121 | 1.0 | 3.4201 | 8.145 | 8.75800 | 90.0 | 90.0 | 90.0 | 1.6350 | Phase III polymorph |
| UREAXX38 | P21212 | 0.5 | 3.40800 | 7.363 | 4.64800 | 90.0 | 90.0 | 90.0 | 1.7100 | Phase IV polymorph |
| UREAXX39 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX40 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX41 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX42 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX43 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX44 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX45 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX46 | P-421m | 0.25 | 5.64300 | 5.64300 | 4.69910 | 90.0 | 90.0 | 90.0 | 1.3328 | polymorph I |
| UREAXX47 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX48 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX49 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX50 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX51 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX52 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX53 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX54 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX55 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX56 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX57 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX58 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX59 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX60 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX61 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX62 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX63 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX64 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX65 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX66 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX67 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX68 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX69 | P-421m | 0.25 | 5.6482 | 5.6482 | 4.7026 | 90.0 | 90.0 | 90.0 | 1.3294 | polymorph I |
| UREAXX70 | P-421m | 0.25 | 5.596 | 5.596 | 4.7164 | 90.0 | 90.0 | 90.0 | 1.3504 | polymorph I |
| UREAXX71 | P-421m | 0.25 | 5.596 | 5.596 | 4.7164 | 90.0 | 90.0 | 90.0 | 1.3504 | polymorph I |
| UREAXX72 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX73 | P-421m | 0.25 | 5.58850 | 5.58850 | 4.6893 | 90.0 | 90.0 | 90.0 | 1.3618 | polymorph I |
| UREAXX74 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX75 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX76 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX77 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX78 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX79 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX80 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX81 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX82 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX83 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX84 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX85 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX86 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |
| UREAXX87 | P-421m | 0.25 | 5.578 | 5.578 | 4.686 | 90.0 | 90.0 | 90.0 | 1.3679 | polymorph I |

Table 2.  Experimental information for CSD entries for Urea.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| UREAXX | P-421m | 5.8 | None | 1961 | 10.1107/S0365110X61002187 |
| UREAXX01 | P-421m | 5.9 | at -140 deg.C | 1961 | 10.1107/S0365110X61002187 |
| UREAXX02 | P-421m | 0.5 | at 148 K | 1999 | 10.1107/S0108768198005746 |
| UREAXX04 | P-421m | 1.5 | 123 K | 1978 | 10.1107/S0567740878006172 |
| UREAXX07 | P-421m | 1.06 | at 123 K | 1980 | 10.1107/S0567740880006693 |
| UREAXX08 | P-421m | 3.0 | at 123 K | 1980 | None |
| UREAXX09 | P-421m | 4.0 | None | 1980 | None |
| UREAXX10 | P-421m | None | at 100 K | 1980 | None |
| UREAXX11 | P-421m | 1.900 | at 60 K | 1980 | None |
| UREAXX12 | P-421m | 2.5 | at 12K | 1984 | 10.1107/S0108768184002135 |
| UREAXX13 | P-421m | 2.5 | at 60 K | 1984 | 10.1107/S0108768184002135 |
| UREAXX14 | P-421m | 2.800 | at 123 K | 1984 | 10.1107/S0108768184002135 |
| UREAXX22 | P-421m | None | None | 1969 | 10.1107/S0567740869002330 |
| UREAXX23 | P-421m | 3.39 | at 293 K | 2005 | None |
| UREAXX24 | P-421m | 6.45 | 296 K | 2009 | 10.1021/jp904942c |
| UREAXX25 | P-421m | 1.04 | 123 K | 2004 | 10.1107/S0108767304015120 |
| UREAXX26 | P21212 | 3.32 | 296 K | 2009 | 10.1021/jp904942c |
| UREAXX27 | P212121 | 3.44 | 296 K | 2009 | 10.1021/jp904942c |
| UREAXX28 | P212121 | 5.38 | 296 K | 2009 | 10.1021/jp904942c |
| UREAXX29 | P-421m | 1.21 | 123 K | 2016 | 10.1126/sciadv.1600192 |
| UREAXX30 | P-421m | 3.53 | 296 K | 2017 | 10.1021/acs.jpcc.6b11454 |
| UREAXX31 | P-421m | 3.0 | 296 K | 2017 | 10.1021/acs.jpcc.6b11454 |
| UREAXX32 | P212121 | 5.390 | 296 K | 2017 | 10.1021/acs.jpcc.6b11454 |
| UREAXX33 | P212121 | 3.95 | 296 K | 2017 | 10.1021/acs.jpcc.6b11454 |
| UREAXX34 | P212121 | 4.88 | 296 K | 2017 | 10.1021/acs.jpcc.6b11454 |
| UREAXX35 | P212121 | 9.99 | 296 K | 2017 | 10.1021/acs.jpcc.6b11454 |
| UREAXX36 | P212121 | 5.81 | 296 K | 2017 | 10.1021/acs.jpcc.6b11454 |
| UREAXX37 | P212121 | 4.04 | 296 K | 2017 | 10.1021/acs.jpcc.6b11454 |
| UREAXX38 | P21212 | 5.36 | 296 K | 2017 | 10.1021/acs.jpcc.6b11454 |
| UREAXX39 | P-421m | 3.139 | 293 K | 2016 | 10.1107/S2053273315024699 |
| UREAXX40 | P-421m | 2.96 | 293 K | 2016 | 10.1107/S2053273315024699 |
| UREAXX41 | P-421m | 4.06 | 293 K | 2016 | 10.1107/S2053273315024699 |
| UREAXX42 | P-421m | 3.51 | 293 K | 2016 | 10.1107/S2053273315024699 |
| UREAXX43 | P-421m | 3.44 | 293 K | 2016 | 10.1107/S2053273315024699 |
| UREAXX44 | P-421m | 3.0 | 293 K | 2016 | 10.1107/S2053273315024699 |
| UREAXX45 | P-421m | 2.570 | 293 K | 2016 | 10.1107/S2053273315024699 |
| UREAXX46 | P-421m | 2.78 | 293 K | 2020 | None |
| UREAXX47 | P-421m | 1.37 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX48 | P-421m | 1.46 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX49 | P-421m | 1.559 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX50 | P-421m | 1.37 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX51 | P-421m | 1.359 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX52 | P-421m | 1.359 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX53 | P-421m | 1.37 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX54 | P-421m | 1.51 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX55 | P-421m | 1.420 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX56 | P-421m | 1.359 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX57 | P-421m | 1.6 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX58 | P-421m | 1.69 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX59 | P-421m | 1.51 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX60 | P-421m | 1.34 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX61 | P-421m | 1.37 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX62 | P-421m | 1.37 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX63 | P-421m | 1.38 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX64 | P-421m | 1.53 | 123 K | 2020 | 10.1107/S2052252520013603 |
| UREAXX65 | P-421m | 1.79 | 123 K | 2020 | 10.1107/S2052520620002917 |
| UREAXX66 | P-421m | 1.71 | 123 K | 2020 | 10.1107/S2052520620002917 |
| UREAXX67 | P-421m | 1.31 | 123 K | 2020 | 10.1107/S2052520620002917 |
| UREAXX68 | P-421m | 1.08 | 123 K | 2020 | 10.1107/S2052520620002917 |
| UREAXX69 | P-421m | 3.980 | 293 K | 2020 | 10.1002/cphc.201901024 |
| UREAXX70 | P-421m | 17.56 | 81 K | 2024 | 10.1107/S2053229624005357 |
| UREAXX71 | P-421m | 16.28 | 81 K | 2024 | 10.1107/S2053229624005357 |
| UREAXX72 | P-421m | 1.17 | 123 K | 2023 | 10.1063/5.0138312 |
| UREAXX73 | P-421m | 2.68 | 150 K | 2024 | 10.1021/acs.jchemed.4c00797 |
| UREAXX74 | P-421m | 1.35 | 123 K | 2025 | 10.1107/S2052252524011242 |
| UREAXX75 | P-421m | 1.35 | 123 K | 2025 | 10.1107/S2052252524011242 |
| UREAXX76 | P-421m | 1.34 | 123 K | 2025 | 10.1107/S2052252524011242 |
| UREAXX77 | P-421m | 1.359 | 123 K | 2025 | 10.1107/S2052252524011242 |
| UREAXX78 | P-421m | 1.38 | 123 K | 2025 | 10.1107/S2052252524011242 |
| UREAXX79 | P-421m | 1.38 | 123 K | 2025 | 10.1107/S2052252524011242 |
| UREAXX80 | P-421m | 0.559 | 123 K | 2025 | 10.1107/S2052252524011242 |
| UREAXX81 | P-421m | 1.34 | 123 K | 2025 | 10.1107/S2052252524011242 |
| UREAXX82 | P-421m | 1.34 | 123 K | 2025 | 10.1107/S2052252524011242 |
| UREAXX83 | P-421m | 1.329 | 123 K | 2025 | 10.1107/S2052252524011242 |
| UREAXX84 | P-421m | 1.35 | 123 K | 2025 | 10.1107/S2052252524011242 |
| UREAXX85 | P-421m | 1.359 | 123 K | 2025 | 10.1107/S2052252524011242 |
| UREAXX86 | P-421m | 0.549 | 123 K | 2025 | 10.1107/S2052252524011242 |
| UREAXX87 | P-421m | 1.37 | 123 K | 2025 | 10.1107/S2052252524011242 |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes

When Steven did the original search, From IV was called Form II.