# 5-Formyluracil

(Last updated June 2026)

Figure 1.  The molecular diagram of 5-Formyluracil.

# CSP studies

| REFCODE | GIMREA |
| --- | --- |
| Formula | C5 H4 N2 O3 |
| Common Name | 5-formyluracil |
| IUPAC Systematic Name | 2,4-dioxo-1,2,3,4-tetrahydropyrimidine-5-carbaldehyde |
| Other Names |  |
| CSD Refcodes | GIMREA |
| Search Identifier | A |
| Scientist | Not sure |
| Date | 2009 |
| Publication | No publication planned. |
| Energy model | 1 |
| Study_ID | 0 |
| Programs | MOLPAK, DMAREL (4.1.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-SolventDatabasesForCrystOpt\5-formyluracil |
| Potential Description | DMA + FIT |
| Intramolecular Description | MP2/6-31G(d,p) |

Figure 2.  Crystal energy landscape of 5-Formyluracil from previous work.

# CSD structures (CSD version 6.01 with Feb 2026 update)

Table 1.  Crystallographic information for CSD entries for 5-Formyluracil.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| GIMREA | Cmc21 | 0.5 | 6.28400 | 6.705 | 12.8302 | 90.0 | 90.0 | 90.0 | 1.7213 | None |

Table 2.  Experimental information for CSD entries for 5-Formyluracil.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| GIMREA | Cmc21 | 4.25 | at 298 K | 2007 | 10.1107/S0108270107045659 |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes