# Chloroform

(Last updated April 2026)

Figure 1.  The molecular diagram of chloroform.

# CSP studies

| REFCODE | CLFORM |
| --- | --- |
| Formula | C1 H1 Cl3 |
| Common Name | Chloroform |
| IUPAC Systematic Name | trichloromethane |
| Other Names |  |
| CSD Refcodes | CLFORM02, CLFORM03 |
| Search Identifier | A |
| Scientist | Not sure |
| Date | pre-2010 |
| Publication | No publication planned. |
| Energy model | 1 |
| Study_ID | 2 |
| Programs | MOLPAK, DMACRYS (2.0.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\Chloroform_aniso |
| Potential Description | MP2 6-31G(d,p) DMA+ANISO (c.f. GMD) |
| Intramolecular Description | MP2 6-31G(d,p) |
| Search Identifier | B |
| Scientist | Not sure |
| Date | pre-2010 |
| Publication | No publication planned. |
| Energy model | 1 |
| Study_ID | 1 |
| Programs | MOLPAK, DMACRYS (2.0.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\Chloroform_charges |
| Potential Description | MP2 6-31G(d,p) Charges+ FIT |
| Intramolecular Description | MP2 6-31G(d,p) |

Figure 2.  Crystal energy landscape of chloroform from previous work.

# CSD structures (CSD version 6.01 with Feb 2026 update)

Table 1.  Crystallographic information for CSD entries for chloroform.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CLFORM | Pnma | 0.5 | 7.485 | 9.497 | 5.841 | 90.0 | 90.0 | 90.0 | 1.9097 | alpha polymorph |
| CLFORM01 | Pnma | 0.5 | 7.4081 | 9.40340 | 5.75400 | 90.0 | 90.0 | 90.0 | 1.9782 | alpha polymorph |
| CLFORM02 | P63 | 0.33 | 5.8868 | 5.8868 | 6.65410 | 90.0 | 90.0 | 120 | 1.9852 | beta polymorph |
| CLFORM03 | Pnma | 0.5 | 7.44220 | 9.4578 | 5.8025 | 90.0 | 90.0 | 90.0 | 1.9414 | alpha polymorph |

Table 2.  Experimental information for CSD entries for chloroform.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| CLFORM | Pnma | 11.0 | at 185 K | 1966 | None |
| CLFORM01 | Pnma | 3.550 | at 293 K | 2008 | 10.1021/jp8020134 |
| CLFORM02 | P63 | 2.95 | at 295 K | 2008 | 10.1021/jp8020134 |
| CLFORM03 | Pnma | 1.72 | at 120 K | 2010 | 10.1039/b914851e |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes