# Imidazole

(Last updated May 2026)

Figure 1.  The molecular diagram of Imidazole.

# CSP studies

| REFCODE | IMAZOL |
| --- | --- |
| Formula | C3 H4 N2 |
| Common Name | Imidazole |
| IUPAC Systematic Name | Imidazole |
| Other Names |  |
| CSD Refcodes | IMAZOL06, IMAZOL25 |
| Search Identifier | A |
| Scientist | Antonio Torrisi |
| Date | 2004 |
| Publication | Price, S. L., Patel, B., Pridhanani-Jethani, P., Torrisi, A., Trans. ACA, 39(2), 1-12 (2004) |
| Energy model | 1 |
| Study_ID | 0 |
| Programs | MOLPAK, DMAREL (3.0) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\imidazole |
| Potential Description | DMA + FIT |
| Intramolecular Description | MP2/6-31G(d,p) |

Figure 2.  Crystal energy landscape of Imidazole from previous work.

# CSD structures (CSD version 6.01 with Feb 2026 update)

Table 1.  Crystallographic information for CSD entries for Imidazole.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| IMAZOL01 | P21/c | 1.0 | 7.582 | 5.371 | 9.79000 | 90.0 | 61.020000 | 90.0 | 1.2965 | alpha polymorph |
| IMAZOL02 | P21/c | 1.0 | 7.746 | 5.447 | 9.75 | 90.0 | 117.5 | 90.0 | 1.2392 | alpha polymorph |
| IMAZOL03 | P21/n | 1.0 | 7.583 | 5.37400 | 9.02700 | 90.0 | 108.71000 | 90.0 | 1.2977 | alpha polymorph |
| IMAZOL04 | P21/c | 1.0 | 7.582 | 5.371 | 9.79000 | 90.0 | 118.98 | 90.0 | 1.2965 | alpha polymorph |
| IMAZOL06 | P21/c | 1.0 | 7.569 | 5.36600 | 9.785 | 90.0 | 119.08 | 90.0 | 1.3018 | alpha polymorph |
| IMAZOL10 | P21/c | 1.0 | 7.7 | 5.43 | 9.73 | 90.0 | 117.33 | 90.0 | 1.2511 | alpha polymorph |
| IMAZOL13 | P21/c | 1.0 | 7.732 | 5.458 | 9.779 | 90.0 | 117.26 | 90.0 | 1.2325 | alpha polymorph |
| IMAZOL14 | P21/n | 1.0 | 7.604 | 5.383 | 9.05600 | 90.0 | 108.876 | 90.0 | 1.2891 | alpha polymorph |
| IMAZOL15 | P21/c | 1.0 | 7.68 | 5.37900 | 9.773 | 90.0 | 118.29000 | 90.0 | 1.2719 | alpha polymorph |
| IMAZOL16 | P21/c | 1.0 | 7.577 | 5.282 | 9.727 | 90.0 | 119.64000 | 90.0 | 1.3364 | alpha polymorph |
| IMAZOL17 | P21/c | 1.0 | 7.503 | 5.202 | 9.688 | 90.0 | 120.54 | 90.0 | 1.3884 | alpha polymorph |
| IMAZOL18 | P21/c | 1.0 | 7.44 | 5.127 | 9.646 | 90.0 | 121.30000 | 90.0 | 1.4382 | alpha polymorph |
| IMAZOL19 | P21/c | 1.0 | 7.41400 | 5.091 | 9.618 | 90.0 | 121.75000 | 90.0 | 1.4647 | alpha polymorph |
| IMAZOL20 | P21/c | 1.0 | 7.36 | 5.035 | 9.574 | 90.0 | 122.25 | 90.0 | 1.5069 | alpha polymorph |
| IMAZOL21 | P21/c | 1.0 | 7.32600 | 4.997 | 9.55600 | 90.0 | 122.68 | 90.0 | 1.5356 | alpha polymorph |
| IMAZOL22 | Aba2 | 1.0 | 14.25 | 8.623 | 5.399 | 90.0 | 90.0 | 90.0 | 1.3631 | beta polymorph |
| IMAZOL23 | Aba2 | 1.0 | 13.914 | 8.603 | 5.335 | 90.0 | 90.0 | 90.0 | 1.4161 | beta polymorph |
| IMAZOL24 | Aba2 | 1.0 | 13.875 | 8.675 | 5.301 | 90.0 | 90.0 | 90.0 | 1.4173 | beta polymorph |
| IMAZOL25 | Aba2 | 1.0 | 13.878 | 8.648 | 5.284 | 90.0 | 90.0 | 90.0 | 1.4260 | beta polymorph |
| IMAZOL26 | Aba2 | 1.0 | 13.817 | 8.624 | 5.287 | 90.0 | 90.0 | 90.0 | 1.4355 | beta polymorph |
| IMAZOL27 | Aba2 | 1.0 | 13.772 | 8.634 | 5.26800 | 90.0 | 90.0 | 90.0 | 1.4437 | beta polymorph |
| IMAZOL28 | Aba2 | 1.0 | 13.773 | 8.635 | 5.2607 | 90.0 | 90.0 | 90.0 | 1.4454 | beta polymorph |
| IMAZOL29 | Aba2 | 1.0 | 13.691 | 8.609 | 5.263 | 90.0 | 90.0 | 90.0 | 1.4578 | beta polymorph |
| IMAZOL30 | Aba2 | 1.0 | 13.61 | 8.624 | 5.242 | 90.0 | 90.0 | 90.0 | 1.4698 | beta polymorph |
| IMAZOL31 | Aba2 | 1.0 | 13.308 | 8.581 | 5.15 | 90.0 | 90.0 | 90.0 | 1.5377 | beta polymorph |
| IMAZOL32 | Aba2 | 1.0 | 13.175 | 8.555 | 5.126 | 90.0 | 90.0 | 90.0 | 1.5652 | beta polymorph |
| IMAZOL33 | Aba2 | 1.0 | 13.074 | 8.521 | 5.102 | 90.0 | 90.0 | 90.0 | 1.5911 | beta polymorph |
| IMAZOL34 | P21/n | 1.0 | 7.72950 | 5.4413 | 9.25940 | 90.0 | 110.54100 | 90.0 | 1.2399 | alpha polymorph |
| IMAZOL35 | P21/n | 1.0 | 7.7485 | 5.46010 | 9.29520 | 90.0 | 110.648 | 90.0 | 1.2287 | alpha polymorph |
| IMAZOL36 | P21/n | 1.0 | 7.7251 | 5.445 | 9.2599 | 90.0 | 110.556 | 90.0 | 1.2398 | alpha polymorph |

Table 2.  Experimental information for CSD entries for Imidazole.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| IMAZOL01 | P21/c | 11.20 | None | 1966 | 10.1107/S0365110X66001853 |
| IMAZOL02 | P21/c | 10.0 | None | 1971 | None |
| IMAZOL03 | P21/n | 6.810 | at 173 K | 1999 | None |
| IMAZOL04 | P21/c | 7.4 | at -150 deg.C | 1977 | neutron, 10.1107/S0567740877008954 |
| IMAZOL06 | P21/c | 2.6 | at 103 K | 1979 | neutron, 10.1107/S0567740879004441 |
| IMAZOL10 | P21/c | 6.4 | None | 1969 | None |
| IMAZOL13 | P21/c | 4.600 | None | 1977 | neutron, 10.1107/S0567740877008954 |
| IMAZOL14 | P21/n | 3.9 | at 173 K | 2008 | None |
| IMAZOL15 | P21/c | 8.2 | at 293 K | 2012 | at 0.15 GPa, 10.1021/cg300852t |
| IMAZOL16 | P21/c | 6.55 | at 293 K | 2012 | at 0.5 GPa, 10.1021/cg300852t |
| IMAZOL17 | P21/c | 5.75 | at 293 K | 2012 | at 0.94 GPa, 10.1021/cg300852t |
| IMAZOL18 | P21/c | 4.850 | at 293 K | 2012 | at 1.41 GPa, 10.1021/cg300852t |
| IMAZOL19 | P21/c | 3.36 | at 293 K | 2012 | at 1.6 GPa, 10.1021/cg300852t |
| IMAZOL20 | P21/c | 4.29 | at 293 K | 2012 | at 2.24 GPa, 10.1021/cg300852t |
| IMAZOL21 | P21/c | 7.32 | at 293 K | 2012 | at 2.7 GPa, 10.1021/cg300852t |
| IMAZOL22 | Aba2 | 6.99 | at 293 K | 2012 | at 0.5 GPa, 10.1021/cg300852t |
| IMAZOL23 | Aba2 | 5.82 | at 293 K | 2012 | at 0.8 GPa, 10.1021/cg300852t |
| IMAZOL24 | Aba2 | 5.71 | at 293 K | 2012 | at 0.8 GPa, 10.1021/cg300852t |
| IMAZOL25 | Aba2 | 4.95 | at 293 K | 2012 | at 0.9 GPa, 10.1021/cg300852t |
| IMAZOL26 | Aba2 | 5.92 | at 293 K | 2012 | at 1.11 GPa, 10.1021/cg300852t |
| IMAZOL27 | Aba2 | 6.28 | at 293 K | 2012 | at 1.2 GPa, 10.1021/cg300852t |
| IMAZOL28 | Aba2 | 5.99 | at 353 K | 2012 | at 1.2 GPa, 10.1021/cg300852t |
| IMAZOL29 | Aba2 | 5.810 | at 293 K | 2012 | at 1.4 GPa, 10.1021/cg300852t |
| IMAZOL30 | Aba2 | 9.42 | at 293 K | 2012 | at 1.6 GPa, 10.1021/cg300852t |
| IMAZOL31 | Aba2 | 8.56 | at 293 K | 2012 | at 2.5 GPa, 10.1021/cg300852t |
| IMAZOL32 | Aba2 | 7.98 | at 293 K | 2012 | at 3.0 GPa, 10.1021/cg300852t |
| IMAZOL33 | Aba2 | 7.3 | at 293 K | 2012 | at 3.35 GPa, 10.1021/cg300852t |
| IMAZOL34 | P21/n | 4.02 | 295 K | 2021 | None |
| IMAZOL35 | P21/n | 4.22 | 296.1 K | 2024 | None |
| IMAZOL36 | P21/n | 6.08 | 299.3 K | 2024 | 10.1016/j.optmat.2024.115964 |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes