# 5-azauracil

(Last updated April 2026)

Figure 1.  The molecular diagram of 5-azauracil.

# CSP studies

| REFCODE | XERBEB |
| --- | --- |
| Formula | C3 H3 N3 O2 |
| Common Name | 5-azauracil |
| IUPAC Systematic Name | 1H-[1,3,5]triazin-2,4-dione |
| Other Names |  |
| CSD Refcodes | XERBEB |
| Search Identifier | A |
| Scientist | Ashley Hulme |
| Date | 2007 |
| Publication | See HOQHAW search |
| Energy model | 1 |
| Study_ID | 0 |
| Programs | MOLPAK, DMAREL (4.1.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\5-azauracil |
| Potential Description | MP2 6-31G(d,p) DMA +FIT |
| Intramolecular Description | MP2 6-31G(d,p) optimized |

Figure 2.  Crystal energy landscape of 5-azauracil from previous work.

# CSD structures (CSD version 6.01 with Feb 2026 update)

Table 1.  Crystallographic information for CSD entries for 5-azauracil.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| XERBEB | Pbca | 1.0 | 6.51350 | 13.5217 | 9.5824 | 90.0 | 90.0 | 90.0 | 1.7798 | None |

Table 2.  Experimental information for CSD entries for 5-azauracil.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| XERBEB | Pbca | 3.37 | None | 1999 | 10.1016/S0022-2860(98)00849-7 |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes