# Pyridone

(Last updated June 2026)

Figure 1.  The molecular diagram of Pyridone.

# CSP studies

| REFCODE | PYRIDO |
| --- | --- |
| Formula | C5 H5 N1 O1 |
| Common Name | 2-Pyridone |
| IUPAC Systematic Name | Pyridin-2(1H)-one |
| Other Names |  |
| CSD Refcodes | PYRIDO04, PYRIDO12 |
| Search Identifier | A |
| Scientist | Not sure |
| Date | 2012 |
| Publication | No publication planned. |
| Energy model | 1 |
| Study_ID | 0 |
| Programs | MOLPAK, DMACRYS (2.0.4) |
| Location on S Drive | \CHEMISTRY_CPOSS\Pyridone\FIT |
| Potential Description | DMA(PBE0/aug-cc-pVTz) + GDMA2 + FIT |
| Intramolecular Description | PBE0/aug-cc-pVTz |
| Search Identifier | B |
| Scientist | Not sure |
| Date | 2012 |
| Publication | No publication planned. |
| Energy model | 1 |
| Study_ID | 1 |
| Programs | MOLPAK, DMACRYS (2.0.4) |
| Location on S Drive | \CHEMISTRY_CPOSS\Pyridone\WILLIAMS |
| Potential Description | DMA(PBE0/aug-cc-pVTz) + GDMA2 + WILLIAMS |
| Intramolecular Description | PBE0/aug-cc-pVTz |

Figure 2.  Crystal energy landscape of Pyridone from previous work.  Left: Energy model A1.  Right: Energy model B1.

# CSD structures (CSD version 6.01 with Feb 2026 update)

Table 1.  Crystallographic information for CSD entries for Pyridone.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PYRIDO | P212121 | 1.0 | 13.63 | 5.89 | 5.67 | 90.0 | 90.0 | 90.0 | 1.3876 | orthorhombic polymorph |
| PYRIDO02 | P212121 | 1.0 | 13.645 | 5.9 | 5.692 | 90.0 | 90.0 | 90.0 | 1.3784 | orthorhombic polymorph |
| PYRIDO03 | P212121 | 1.0 | 13.564 | 5.792 | 5.598 | 90.0 | 90.0 | 90.0 | 1.4362 | orthorhombic polymorph |
| PYRIDO04 | P212121 | 1.0 | 13.564 | 5.795 | 5.604 | 90.0 | 90.0 | 90.0 | 1.4339 | orthorhombic polymorph |
| PYRIDO05 | P212121 | 1.0 | 13.585 | 5.806 | 5.603 | 90.0 | 90.0 | 90.0 | 1.4293 | orthorhombic polymorph |
| PYRIDO11 | P212121 | 1.0 | 13.657 | 5.912 | 5.70100 | 90.0 | 90.0 | 90.0 | 1.3722 | orthorhombic polymorph |
| PYRIDO12 | P21/n | 2.0 | 6.2027 | 16.327 | 9.1046 | 90.0 | 92.242 | 90.0 | 1.3711 | monoclinic polymorph |
| PYRIDO13 | P212121 | 1.0 | 5.613 | 5.80840 | 13.5959 | 90.0 | 90.0 | 90.0 | 1.4250 | orthorhombic polymorph |

Table 2.  Experimental information for CSD entries for Pyridone.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| PYRIDO | P212121 | 6.7 | None | 1953 | 10.1107/S0365110X5300168X |
| PYRIDO02 | P212121 | 3.9 | None | 1984 | None |
| PYRIDO03 | P212121 | 4.1 | at 120 K | 1984 | None |
| PYRIDO04 | P212121 | 2.6 | at 120 K | 1984 | None |
| PYRIDO05 | P212121 | 4.0 | at 123 K | 1998 | 10.1107/S0108768198006545 |
| PYRIDO11 | P212121 | 3.4 | None | 1984 | None |
| PYRIDO12 | P21/n | 4.4 | at 98 K | 2009 | 10.1107/S1600536809049496 |
| PYRIDO13 | P212121 | 2.719 | 123 K | 2024 | 10.1002/chir.23617 |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes