# Tetrolic Acid

(Last updated June 2026)

Figure 1.  The molecular diagram of Tetrolic Acid.

# CSP studies

| REFCODE | TETROL |
| --- | --- |
| Formula | C4 H4 O2 |
| Common Name | Tetrolic Acid |
| IUPAC Systematic Name | But-2-ynoic Acid |
| Other Names |  |
| CSD Refcodes | TETROL02, TETROL07 |
| Search Identifier | A |
| Scientist | Matthew Habgood |
| Date | 2012 |
| Publication | Habgood M 2012. Phys Chem Chem Phys 14, 9195-9203. |
| Energy model | 1 |
| Study_ID | 30 |
| Programs | Rigid CrystalPredictor, DMACRYS (2.0.4) |
| Location on S Drive | \CHEMISTRY_CPOSS\TetrolicAcid\PCM |
| Potential Description | GDMA2.2(PCMdielectric3(MP2/6-31G(d,p))) + FIT with a increased by 1.1 and c increased by 1.25 |
| Intramolecular Description | MP2/6-31G(d,p) |
| Energy model | 2 |
| Study_ID | 10 |
| Programs | Study_ID=30, CrystalOptimizer, DMACRYS (2.0.4) |
| Location on S Drive | \CHEMISTRY_CPOSS\TetrolicAcid\CrystOpt |
| Potential Description | CrystalOptimizer, GDMA2.2(MP2/6-31G(d,p)) + FIT |
| Intramolecular Description | PBE0(6-31G(d,p)) |

Figure 2.  Crystal energy landscape of Tetrolic Acid from previous work.  Left: Energy model A1.  Right: Energy model A2.

# CSD structures (CSD version 6.01 with Feb 2026 update)

Table 1.  Crystallographic information for CSD entries for Tetrolic Acid.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TETROL | P-1 | 1.0 | 7.32 | 5.099 | 7.226 | 83.91 | 117.46 | 112.0 | 1.2624 | alpha polymorph |
| TETROL01 | P21 | 1.0 | 7.887 | 7.121 | 3.937 | 90.0 | 100.18 | 90.0 | 1.2829 | beta polymorph |
| TETROL02 | P-1 | 1.0 | 5.0156 | 6.9262 | 7.0836 | 112.956 | 97.227 | 107.388 | 1.3433 | triclinic P-1 polymorph |
| TETROL03 | P-1 | 1.0 | 5.0359 | 6.9758 | 7.1152 | 112.963 | 97.033 | 107.706 | 1.3245 | triclinic P-1 polymorph |
| TETROL04 | P-1 | 1.0 | 5.058 | 7.0169 | 7.1325 | 112.92 | 96.962 | 108.002 | 1.3099 | triclinic P-1 polymorph |
| TETROL05 | P-1 | 1.0 | 5.0673 | 7.0638 | 7.163 | 113.064 | 96.689 | 108.347 | 1.2968 | triclinic P-1 polymorph |
| TETROL06 | P21 | 1.0 | 3.91580 | 7.1104 | 7.871 | 90.0 | 100.59 | 90.0 | 1.2961 | monoclinic P21 polymorph |
| TETROL07 | P21 | 1.0 | 3.8248 | 7.0987 | 7.7801 | 90.0 | 101.058 | 90.0 | 1.3467 | monoclinic P21 polymorph |
| TETROL08 | P21 | 1.0 | 3.85180 | 7.0956 | 7.79240 | 90.0 | 100.862 | 90.0 | 1.3349 | monoclinic P21 polymorph |
| TETROL09 | P21 | 1.0 | 3.8856 | 7.1138 | 7.8353 | 90.0 | 100.93 | 90.0 | 1.3130 | monoclinic P21 polymorph |
| TETROL10 | P21 | 1.0 | 3.8912 | 7.11410 | 7.8453 | 90.0 | 100.8 | 90.0 | 1.3088 | monoclinic P21 polymorph |
| TETROL11 | P21 | 1.0 | 3.9127 | 7.1074 | 7.8489 | 90.0 | 100.422 | 90.0 | 1.3006 | monoclinic P21 polymorph |
| TETROL12 | P21 | 1.0 | 3.9417 | 7.1096 | 7.878 | 90.0 | 100.25 | 90.0 | 1.2852 | monoclinic P21 polymorph |

Table 2.  Experimental information for CSD entries for Tetrolic Acid.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| TETROL | P-1 | 7.0 | None | 1972 | 10.1039/p29720001763 |
| TETROL01 | P21 | 4.0 | None | 1972 | 10.1039/p29720001763 |
| TETROL02 | P-1 | 5.38 | 118 K | 2015 | 10.1039/C5NJ00196J |
| TETROL03 | P-1 | 5.75 | 154 K | 2015 | 10.1039/C5NJ00196J |
| TETROL04 | P-1 | 6.4 | 190 K | 2015 | 10.1039/C5NJ00196J |
| TETROL05 | P-1 | 6.05 | 226 K | 2015 | 10.1039/C5NJ00196J |
| TETROL06 | P21 | 6.33 | 262 K | 2015 | 10.1039/C5NJ00196J |
| TETROL07 | P21 | 4.0 | 118 K | 2015 | 10.1039/C5NJ00196J |
| TETROL08 | P21 | 4.26 | 154 K | 2015 | 10.1039/C5NJ00196J |
| TETROL09 | P21 | 4.36 | 190 K | 2015 | 10.1039/C5NJ00196J |
| TETROL10 | P21 | 4.64 | 226 K | 2015 | 10.1039/C5NJ00196J |
| TETROL11 | P21 | 4.600 | 262 K | 2015 | 10.1039/C5NJ00196J |
| TETROL12 | P21 | 5.13 | 298 K | 2015 | 10.1039/C5NJ00196J |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes