# 5-Fluorocytosine

(Last updated May 2026)

Figure 1.  The molecular diagram of 5-Fluorocytosine.

# CSP studies

| REFCODE | MEBQEQ |
| --- | --- |
| Formula | C4 H4 N3 O1 F1 |
| Common Name | Fluorocytosine |
| IUPAC Systematic Name | 5-fluorocytosine |
| Other Names |  |
| CSD Refcodes | MEBQEQ, MEBQEQ01 |
| Search Identifier | A |
| Scientist | Ashley Hulme |
| Date | 2006 |
| Publication | Hulme, A. T.; Tocher, D. A. Cryst. Growth Des. 6(2), 481-487 (2006) |
| Energy model | 1 |
| Study_ID | 0 |
| Programs | MOLPAK, DMAREL (4.1.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\fluorocytosine |
| Potential Description | DMA + FIT + Williams F parameters |
| Intramolecular Description | Ab initio MP2 |

Figure 2.  Crystal energy landscape of 5-Fluorocytosine from previous work.

# CSD structures (CSD version 6.01 with Feb 2026 update)

Table 1.  Crystallographic information for CSD entries for 5-Fluorocytosine.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MEBQEQ | P21/n | 1.0 | 4.0629 | 9.5211 | 12.7386 | 90.0 | 92.986 | 90.0 | 1.7424 | polymorph II |
| MEBQEQ01 | P41212 | 1.0 | 6.6387 | 6.6387 | 23.471 | 90.0 | 90.0 | 90.0 | 1.6578 | polymorph I |

Table 2.  Experimental information for CSD entries for 5-Fluorocytosine.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| MEBQEQ | P21/n | 3.41 | at 150 K | 2006 | 10.1021/cg050398g |
| MEBQEQ01 | P41212 | 3.34 | at 150 K | 2006 | 10.1021/cg050398g |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes