# 2,9-diiodoanthanthrone (Blind Test IX)

(Last updated March 2026)

Figure 1.  The molecular diagram of 2,9-diiodoanthanthrone.

# CSP studies

| REFCODE | XATMIP |
| --- | --- |
| Formula | C22 H8 O2 I2 |
| Common Name | 2,9-di-iodo-anthathrone |
| IUPAC Systematic Name | 4,10-diiododibenzo[def.mno]chrysene-6,12-dione |
| Other Names |  |
| CSD Refcodes | XATMIP |
| Search Identifier | A |
| Scientist | Sally Price |
| Date | 2005 |
| Publication | Day GM et al, Acta Cryst. B 2005, 61 (5), 511-527 |
| Energy model | 1 |
| Study_ID | 0 |
| Programs | MOLPAK, DMAREL (3.11) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\2,9-diiodoanthanthrone |
| Potential Description | DMA FIT+Halgren mmff I potential |
| Intramolecular Description | SCF 6-311G** |

Figure 2.  Crystal energy landscape of 2,9-diiodoanthanthrone from previous work.

# CSD structures (CSD version 6.01)

Table 1.  Crystallographic information for CSD entries for 2,9-diiodoanthanthrone.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| XATMIP | P21/c | 0.5 | 4.202 | 20.956 | 9.276 | 90.0 | 100.63 | 90.0 | 2.3088 | None |
| XATMIP01 | P21/c | 0.5 | 4.202 | 20.956 | 9.276 | 90.0 | 100.63 | 90.0 | 2.3088 | None |

Table 2.  Experimental information for CSD entries for 2,9-diiodoanthanthrone.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| XATMIP | P21/c | 3.550 | at 293 K | 2005 | 10.1107/S0108768105016563 |
| XATMIP01 | P21/c | 4.17 | at 293 K | 2010 | 10.1107/S0108768110028247 |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes

The search uploaded to the database only contains 35 structures, yet the experimental structure was found about 40th in the search.  Two structures, XATMIP_opt_aa1 and XATMIP_opt_dc25, overlay a sheet with the experimental structure.