# Phenanthrenol

(Last updated May 2026)

Figure 1.  The molecular diagram of Phenanthrenol.

# CSP studies

| REFCODE | CUTCAW |
| --- | --- |
| Formula | C14 H10 O1 |
| Common Name | Phenanthrenol |
| IUPAC Systematic Name | Phenanthren-9-ol |
| Other Names |  |
| CSD Refcodes | CUTCAW |
| Search Identifier | A |
| Scientist | Panos Karamertzanis |
| Date | 2009 |
| Publication | Friscic T, Lancaster RW, Fabian L, Karamertzanis PG PNAS 2010, 107 (30), 13216-13221 |
| Energy model | 2 |
| Study_ID | 10 |
| Programs | Study_ID=20, CrystalOptimizer, DMACRYS (1.1.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\Steroids\phenanthrenol\dmaflex |
| Potential Description | CrystalOptimizer with 13 torsion and 1 bond angles optimised. FIT potential and B3LYP inter and intra levels. |
| Intramolecular Description | B3LYP |
| Energy model | 1 |
| Study_ID | 20 |
| Programs | Rigid CrystalPredictor, DMACRYS (1.1.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\Steroids\phenanthrenol\rigid |
| Potential Description | FIT potential and B3LYP6-31G(d,p) DMA. |
| Intramolecular Description | B3LYP/6-31Gd,p |

Figure 2.  Crystal energy landscape of Phenanthrenol from previous work.

# CSD structures (CSD version 6.01 with Feb 2026 update)

Table 1.  Crystallographic information for CSD entries for Phenanthrenol.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CUTCAW | P212121 | 1.0 | 4.68187 | 12.3504 | 16.7658 | 90.0 | 90.0 | 90.0 | 1.3307 | None |

Table 2.  Experimental information for CSD entries for Phenanthrenol.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| CUTCAW | P212121 | 3.99 | at 298 K | 2010 | 10.1073/pnas.0915142107 |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes