# Pyrene

(Last updated May 2026)

Figure 1.  The molecular diagram of Pyrene.

# CSP studies

| REFCODE | PYRENE |
| --- | --- |
| Formula | C16 H10 |
| Common Name | Pyrene |
| IUPAC Systematic Name | Pyrene |
| Other Names |  |
| CSD Refcodes | PYRENE11, PYRENE06, PYRENE08, PYRENE24, PYRENE29 |
| Search Identifier | A |
| Scientist | Panos Karamertzanis |
| Date | 2009 |
| Publication | Friscic T, Lancaster RW, Fabian L, Karamertzanis PG PNAS 2010, 107 (30), 13216-13221 |
| Energy model | 2 |
| Study_ID | 10 |
| Programs | Study_ID=20, CrystalOptimizer, DMACRYS (2.0.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\Steroids\pyrene\dmaflex |
| Potential Description | CrystalOptimizer with 13 torsion angles optimised. FIT potential and B3LYP inter and intra levels. |
| Intramolecular Description | B3LYP |
| Energy model | 1 |
| Study_ID | 20 |
| Programs | Rigid CrystalPredictor, DMACRYS (2.0.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\Steroids\pyrene\rigid |
| Potential Description | B3LYP DMA + FIT potential. |
| Intramolecular Description | B3LYP |

Figure 2.  Crystal energy landscape of Pyrene from previous work.

# CSD structures (CSD version 6.01 with Feb 2026 update)

Form I and II are very similar.  They overlay with default options, so we don’t expect to see both in the search.

Table 1.  Crystallographic information for CSD entries for Pyrene.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DAFPOU | P21/c | 1 | 8.1431 | 9.8639 | 12.1136 | 90 | 96.484 | 90 | 1.39 | II |
| PYRENE | P21/a | 1 | 13.649 | 9.256 | 8.47 | 90 | 100.28 | 90 | 1.276 | I |
| PYRENE01 | P21/a | 1 | 13.649 | 9.253 | 8.47 | 90 | 100.28 | 90 | 1.276 | I |
| PYRENE02 | P21/a | 1 | 13.649 | 9.256 | 8.47 | 90 | 100.28 | 90 | 1.276 | I |
| PYRENE03 | P21/a | 1 | 13.532 | 9.159 | 8.387 | 90 | 100.25 | 90 | 1.313 | I |
| PYRENE04 | P21/a | 1 | 13.667 | 9.267 | 8.479 | 90 | 100.25 | 90 | 1.271 | I |
| PYRENE05 | P21/a | 1 | 13.644 | 9.255 | 8.469 | 90 | 100.27 | 90 | 1.277 | I |
| PYRENE06 | P21/a | 1.0 | 12.3026 | 9.98788 | 8.22064 | 90.0 | 96.4046 | 90.0 | 1.3382 | II |
| PYRENE07 | P21/a | 1 | 12.358 | 10.02 | 8.26 | 90 | 96.48 | 90 | 1.322 | II |
| PYRENE08 | P21/a | 0.5 | 15.35 | 3.852 | 8.65 | 90 | 103.3 | 90 | 1.35 | III |
| PYRENE09 | P21/a | 0.5 | 15.309 | 3.8375 | 8.3341 | 90 | 102.606 | 90 | 1.406 | III |
| PYRENE10 | P21/c | 1 | 8.374 | 9.144 | 13.502 | 90 | 100.245 | 90 | 1.32 | I |
| PYRENE11 | P21/c | 1 | 8.3726 | 9.1301 | 13.5283 | 90 | 100.281 | 90 | 1.32 | I |
| PYRENE12 | P21/c | 1 | 8.463 | 9.252 | 13.644 | 90 | 100.33 | 90 | 1.278 | I |
| PYRENE13 | P21/c | 1 | 8.3688 | 9.14 | 13.487 | 90 | 100.234 | 90 | 1.323 | I |
| PYRENE14 | P21/a | 1 | 13.651 | 9.257 | 8.472 | 90 | 100.292 | 90 | 1.275 | I |
| PYRENE15 | P21/c | 1 | 8.4032 | 9.1686 | 13.5345 | 90 | 100.317 | 90 | 1.309 | I |
| PYRENE16 | P21/c | 1 | 8.478 | 9.2652 | 13.655 | 90 | 100.31 | 90 | 1.273 | I |
| PYRENE17 | P21/c | 1 | 8.41463 | 9.17935 | 13.5575 | 90 | 100.3116 | 90 | 1.304 | I |
| PYRENE18 | P21/c | 1 | 8.4826 | 9.2796 | 13.638 | 90 | 100.473 | 90 | 1.273 | I |
| PYRENE19 | P21/c | 1 | 8.4679 | 9.2573 | 13.6511 | 90 | 100.256 | 90 | 1.276 | I |
| PYRENE20 | P21/c | 1 | 8.5 | 9.3 | 13.6 | 90 | 100.3 | 90 | 1.27 | I |
| PYRENE21 | P21/c | 1 | 7.0174 | 5.645 | 15.3477 | 90 | 100.363 | 90 | 2.246 | V |
| PYRENE22 | P21/c | 1 | 6.9711 | 5.541 | 15.2471 | 90 | 100.349 | 90 | 2.319 | V |
| PYRENE23 | P21/c | 1 | 8.0322 | 9.7422 | 11.8112 | 90 | 96.074 | 90 | 1.462 | II |
| PYRENE24 | P-1 | 2 | 7.593 | 10.223 | 11.192 | 92.536 | 95.04 | 91.21 | 1.554 | IV |
| PYRENE25 | P-1 | 2 | 7.477 | 10.07 | 10.879 | 92.434 | 94.73 | 90.86 | 1.647 | IV |
| PYRENE26 | P21/c | 1 | 7.45 | 6.4503 | 16.096 | 90 | 100.65 | 90 | 1.767 | V |
| PYRENE27 | P21/c | 1 | 7.345 | 6.2802 | 15.9325 | 90 | 100.57 | 90 | 1.859 | V |
| PYRENE28 | P21/c | 1 | 7.2292 | 6.0333 | 15.759 | 90 | 100.516 | 90 | 1.988 | V |
| PYRENE29 | P21/c | 1 | 7.155 | 5.8939 | 15.6277 | 90 | 100.467 | 90 | 2.073 | V |
| PYRENE30 | P21/c | 1 | 7.0634 | 5.7352 | 15.4503 | 90 | 100.395 | 90 | 2.182 | V |

Table 2.  Experimental information for CSD entries for Pyrene.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| DAFPOU | P21/c | 6.82 | 293 | 2024 | synchrotron, 0.7 GPa, 10.1038/s42004-024-01294-0 |
| PYRENE | P21/a | 11 | 295 | 1965 | 10.1107/S0365110X65001494 |
| PYRENE01 | P21/a | 4.4 | 295 | 1970 | None |
| PYRENE02 | P21/a | 3.2 | 295 | 1972 | neutron, 10.1107/S0567740872007319 |
| PYRENE03 | P21/a | 6.3 | 113 | 1978 | 10.1107/S0567740878005312 |
| PYRENE04 | P21/a | 0 | 295 | 1978 |  |
| PYRENE05 | P21/a | 0 | 295 | 1981 |  |
| PYRENE06 | P21/a | 2.69 | at 4.2 K | 1996 | 10.1016/0009-2614(96)00670-7 |
| PYRENE07 | P21/a | 5.15 | 93 | 2000 | 10.1016/S0022-2860(99)00280-X |
| PYRENE08 | P21/a | 11.82 | 298 | 2006 | 0.3 GPa, 10.1107/S0108768106026814 |
| PYRENE09 | P21/a | 13.36 | 298 | 2006 | 0.5 GPa, 10.1107/S0108768106026814 |
| PYRENE10 | P21/c | 4.13 | 90 | 2016 | 10.1002/chem.201602188 |
| PYRENE11 | P21/c | 4.08 | 100 | 2020 | 10.1039/D0QM00229A |
| PYRENE12 | P21/c | 4.23 | 293 | 2018 | 10.1002/adom.201800198 |
| PYRENE13 | P21/c | 4.6 | 110 | 2015 | 10.1021/acs.cgd.5b00844 |
| PYRENE14 | P21/a | 0 | 0 | 2001 |  |
| PYRENE15 | P21/c | 3.85 | 293 | 2023 | None |
| PYRENE16 | P21/c | 4.86 | 293 | 2024 | synchrotron, 10.1038/s42004-024-01294-0 |
| PYRENE17 | P21/c | 3.77 | 170 | 2025 | 10.1002/anie.202417868 |
| PYRENE18 | P21/c | 6.27 | 293 | 2025 | 10.1016/j.xinn.2025.100884 |
| PYRENE19 | P21/c | 5.64 | 293 | 2025 | 10.1002/adma.202419981 |
| PYRENE20 | P21/c | 24.33 | 298 | 2025 | electron diffraction, 10.1107/S1600576725009823 |
| PYRENE21 | P21/c | 13.62 | 293 | 2024 | synchrotron, 10.1038/s42004-024-01294-0 |
| PYRENE22 | P21/c | 16.55 | 293 | 2024 | synchrotron, 10.1038/s42004-024-01294-0 |
| PYRENE23 | P21/c | 6.14 | 293 | 2024 | synchrotron, 1.4 GPa, 10.1038/s42004-024-01294-0 |
| PYRENE24 | P-1 | 9.77 | 293 | 2024 | synchrotron, 2.7 GPa, 10.1038/s42004-024-01294-0 |
| PYRENE25 | P-1 | 13.41 | 293 | 2024 | synchrotron, 4.3 GPa, 10.1038/s42004-024-01294-0 |
| PYRENE26 | P21/c | 8.65 | 293 | 2024 | synchrotron, 7.3 GPa, 10.1038/s42004-024-01294-0 |
| PYRENE27 | P21/c | 11.66 | 293 | 2024 | synchrotron, 9.5 GPa, 10.1038/s42004-024-01294-0 |
| PYRENE28 | P21/c | 7.78 | 293 | 2024 | synchrotron, 15.4 GPa, 10.1038/s42004-024-01294-0 |
| PYRENE29 | P21/c | 7.55 | 293 | 2024 | synchrotron, 20.2 GPa, 10.1038/s42004-024-01294-0 |
| PYRENE30 | P21/c | 13.56 | 293 | 2024 | synchrotron, 25.2 GPa, 10.1038/s42004-024-01294-0 |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes