# Amantadine Hydrochloride

(Last updated May 2026)

Figure 1.  The molecular diagram of Amantadine Hydrochloride.

# CSP studies

| REFCODE | FINVAZ |
| --- | --- |
| Formula | C10 H18 N1 + Cl1 - |
| Common Name | Amantadine hydrochloride |
| IUPAC Systematic Name | Amantadine hydrochloride |
| Other Names |  |
| CSD Refcodes | FINVAZ01 |
| Search Identifier | A |
| Scientist | Sharmarke Mohamed |
| Date | pre-2010 |
| Publication | No publication planned. |
| Energy model | 1 |
| Study_ID | 20 |
| Programs | Rigid CrystalPredictor, DMACRYS (2.0.2) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\amantadine_hydrochloride |
| Potential Description | DMA(MP2 6-31(d,p)) + WILL01 + Hejczyk chlorine parameters |
| Intramolecular Description | MP2/6-31G(d,p) |

Figure 2.  Crystal energy landscape of Amantadine Hydrochloride from previous work.

# CSD structures (CSD version 6.01 with Feb 2026 update)

Table 1.  Crystallographic information for CSD entries for Amantadine Hydrochloride.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FINVAZ | C2/c | 1.0 | 20.549 | 11.138 | 9.658 | 90.0 | 108.81 | 90.0 | 1.1917 | None |
| FINVAZ01 | C2/c | 1.0 | 20.7095 | 11.1664 | 9.7217 | 90.0 | 109.021 | 90.0 | 1.1732 | None |

Table 2.  Experimental information for CSD entries for Amantadine Hydrochloride.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| FINVAZ | C2/c | 6.5 | at 143 K | 1987 | 10.1107/S010827018709423X |
| FINVAZ01 | C2/c | 4.52 | 100 K | 2022 | 10.1016/j.cherd.2022.09.049 |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes