# (S)-(+)-5-Hydroxymethyl-2-oxazolidinone

(Last updated April 2026)

Figure 1.  The molecular diagram of (S)-(+)-5-Hydroxymethyl-2-oxazolidinone.

# CSP studies

| REFCODE | EXEVUY |
| --- | --- |
| Formula | C4 H7 N1 O3 |
| Common Name | (S)-(+)-5-Hydroxymethyl-2-oxazolidinone |
| IUPAC Systematic Name | (S)-(+)-5-Hydroxymethyl-2-oxazolidinone |
| Other Names |  |
| CSD Refcodes | EXEVUY |
| Search Identifier | A |
| Scientist | Emiliana D'Oria |
| Date | pre-2010 |
| Publication | No publication planned. |
| Energy model | 2 |
| Study_ID | 10 |
| Programs | Study_ID=0, dmaflex (2), DMACRYS (1.1.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\Hydroxymethyloxazolidinone\dmaflex |
| Potential Description | DMA + FIT |
| Intramolecular Description | HF/6-31G(d,p) |
| Energy model | 1 |
| Study_ID | 0 |
| Programs | MOLPAK, DMAREL (4.1.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\Hydroxymethyloxazolidinone\ConOpt |
| Potential Description | DMA + FIT |
| Intramolecular Description | MP2/6-31G(d,p) |

Figure 2.  Crystal energy landscape of (S)-(+)-5-Hydroxymethyl-2-oxazolidinone from previous work.

# CSD structures (CSD version 6.01 with Feb 2026 update)

Table 1.  Crystallographic information for CSD entries for (S)-(+)-5-Hydroxymethyl-2-oxazolidinone.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| EXEVUY | P21 | 1.0 | 5.566 | 7.90020 | 6.2428 | 90.0 | 104.98 | 90.0 | 1.4665 | None |

Table 2.  Experimental information for CSD entries for (S)-(+)-5-Hydroxymethyl-2-oxazolidinone.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| EXEVUY | P21 | 3.04 | at 293 K | 2004 | 10.1016/j.tetasy.2004.03.038 |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes