# Oxamic Acid

(Last updated June 2026)

Figure 1.  The molecular diagram of Oxamic Acid.

# CSP studies

| REFCODE | AFIGOO |
| --- | --- |
| Formula | C2 H3 N1 O3 |
| Common Name | Oxamic acid |
| IUPAC Systematic Name | Oxalamic acid |
| Other Names | Oxalic acid monoamide, Aminooxoacetic acid |
| CSD Refcodes | AFIGOO |
| Search Identifier | A |
| Scientist | Not sure |
| Date | pre-2010 |
| Publication | No publication planned. |
| Energy model | 1 |
| Study_ID | 0 |
| Programs | MOLPAK, DMAREL (4.1.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\oxamic_acid |
| Potential Description | DMA + FIT |
| Intramolecular Description | MP2/6-31G(d,p) |

Figure 2.  Crystal energy landscape of Oxamic Acid from previous work.

# CSD structures (CSD version 6.01 with Feb 2026 update)

Table 1.  Crystallographic information for CSD entries for Oxamic Acid.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| AFIGOO | Cc | 1.0 | 9.4989 | 5.43796 | 6.86370 | 90.0 | 107.15200 | 90.0 | 1.7459 | None |
| AFIGOO01 | Cc | 1.0 | 9.4994 | 5.43800 | 6.8636 | 90.0 | 107.149 | 90.0 | 1.7458 | None |

Table 2.  Experimental information for CSD entries for Oxamic Acid.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| AFIGOO | Cc | 3.27 | 298 K | 2019 | 10.1016/j.molstruc.2018.09.089 |
| AFIGOO01 | Cc | 8.887 | 298 K | 2023 | None |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes