# Bipyridine Succinic Acid Cocrystal

(Last updated April 2026)

Figure 1.  The molecular diagram of Bipyridine and Succinic Acid.

# CSP studies

| REFCODE | LATJAT |
| --- | --- |
| Formula | C10 N2 H8 - C4 O4 H6 |
| Common Name | Bipyridine - Succinic Acid cocrystal |
| IUPAC Systematic Name | 2,2'-Bipyridyl - Butan-1,4-dioic acid |
| Other Names |  |
| CSD Refcodes | LATJAT |
| Search Identifier | A |
| Scientist | Nizar Issa / Panos Karamertzanis |
| Date | 2012 |
| Publication | Issa N, Barnett SA, Mohamed S, Braun DE, Copley RCB, Tocher DA, Price SL 2012. CrystEngComm 14, 2454-2464. |
| Energy model | 2 |
| Study_ID | 10 |
| Programs | Study_ID=20, CrystalOptimizer, DMACRYS (2.0.2) |
| Location on S Drive | \CHEMISTRY_CPOSS\SuccinicAcidCocrystals\Bipyridine_SuccinicAcid_CO |
| Potential Description | CrystalOptimizer HF/6-31G(d,p) Intra, GDMA2.2(MP2/6-31G(d,p)) DMA + FIT |
| Intramolecular Description | HF/6-31G(d,p) |
| Energy model | 1 |
| Study_ID | 20 |
| Programs | Rigid CrystalPredictor (1), DMACRYS (2.0.2) |
| Location on S Drive | \CHEMISTRY_CPOSS\SuccinicAcidCocrystals\Bipyridine_SuccinicAcid |
| Potential Description | Rigid CrystalPredictor + MP2 6-31G(d,p) DMA +FIT |
| Intramolecular Description | MP2/6-31G(d,p) |

Figure 2.  Crystal energy landscape of the Bipyridine and Succinic Acid cocrystal from previous work.

# CSD structures (CSD version 6.01 with Feb 2026 update)

Table 1.  Crystallographic information for CSD entries for the Bipyridine and Succinic Acid cocrystal.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LATJAT | P21/c | 0.5 | 8.958 | 5.1788 | 14.3570 | 90.0 | 106.10900 | 90.0 | 1.4234 | None |

Table 2.  Experimental information for CSD entries for the Bipyridine and Succinic Acid cocrystal.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| LATJAT | P21/c | 3.91 | at 150 K | 2012 | 10.1039/c2ce06325e |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes