# 1,3-Dibromo-2-chloro-5-fluorobenzene (Blind Test XIII)

(Last updated February 2026)

Figure 1.  The molecular diagram of Dibromo-2-chloro-5-fluorobenzene.

# CSP studies

It was a MOLPAK search, but I’m not sure what xx packing type referred to.

| REFCODE | SOXLEX |
| --- | --- |
| Formula | C6 H2 Br2 Cl1 F1 |
| Common Name | Blind Test XIII |
| IUPAC Systematic Name | 1,3-Dibromo-2-chloro-5-fluorobenzene |
| Other Names |  |
| CSD Refcodes | SOXLEX |
| Search Identifier | A |
| Scientist | Gareth Welch, Alston Misquitta |
| Date | 2008 |
| Publication | Day GM, 2009. Acta Crystallogr, Sect B 65, 107-125; Misquitta AJ, Welch GWA, Stone AJ, Price SL 2008. Chem Phys Lett 456, 105-109. |
| Energy model | 1 |
| Study_ID | 0 |
| Programs | MOLPAK, DMAREL (4.1.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\BlindTestXIII |
| Potential Description | Specific PBE0/Sadlej GDMA2 DMA +dispersion, SAPT fitted anisotropic Repulsion 8a_5 |
| Intramolecular Description | MP2 6-31G(d,p) |

Figure 2.  Crystal energy landscape of Dibromo-2-chloro-5-fluorobenzene from previous work.

# CSD structures (CSD version 6.01)

Table 1.  Crystallographic information for CSD entries for Dibromo-2-chloro-5-fluorobenzene.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SOXLEX | P21/c | 1.0 | 3.89280 | 13.5064 | 14.422 | 90.0 | 93.688 | 90.0 | 2.5309 | None |
| SOXLEX01 | P21/c | 1.0 | 3.89430 | 13.5109 | 14.4296 | 90.0 | 93.636 | 90.0 | 2.5276 | None |

Table 2.  Experimental information for CSD entries for Dibromo-2-chloro-5-fluorobenzene.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| SOXLEX | P21/c | 2.82 | at 173 K | 2008 | None |
| SOXLEX01 | P21/c | 3.6 | 173 K | 2009 | 10.1107/S0108768109004066 |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes