# Propenal

(Last updated March 2026)

Figure 1.  The molecular diagram of Propenal.

# CSP studies

| REFCODE | AXOSOW |
| --- | --- |
| Formula | C3 H4 O1 |
| Common Name | Propenal |
| IUPAC Systematic Name | Propenal |
| Other Names |  |
| CSD Refcodes | AXOSOW |
| Search Identifier | A |
| Scientist | Unknown |
| Date | 2008 |
| Publication | Day GM, 2009. Acta Crystallogr , Sect B 65, 107-125. |
| Energy model | 1 |
| Study_ID | 0 |
| Programs | MOLPAK, DMAREL (4.1.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\BlindTestXII\fit |
| Potential Description | DMA + FIT |
| Intramolecular Description | MP2/6-31G(d,p) |
| Search Identifier | B |
| Scientist | Unknown |
| Date | 2008 |
| Publication | See Study_ID=0 |
| Energy model | 1 |
| Study_ID | 1 |
| Programs | MOLPAK, DMAREL (4.3.6) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\BlindTestXII\williams |
| Potential Description | DMA + Williams99 |
| Intramolecular Description | MP2/6-31G(d,p) |

Figure 2.  Crystal energy landscape of Propenal from previous work.

# CSD structures (CSD version 6.01)

Table 1.  Crystallographic information for CSD entries for Propenal.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| AXOSOW | Pbca | 1.0 | 7.134 | 9.694 | 9.93 | 90.0 | 90.0 | 90.0 | 1.0845 | None |
| AXOSOW01 | Pbca | 1.0 | 6.97 | 9.514 | 9.752 | 90.0 | 90.0 | 90.0 | 1.1516 | None |
| AXOSOW03 | Pbca | 1.0 | 6.97 | 9.514 | 9.752 | 90.0 | 90.0 | 90.0 | 1.1516 | None |

Table 2.  Experimental information for CSD entries for Propenal.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| AXOSOW | Pbca | 3.5 | at 133 K | 2011 | 10.1039/c0cp02236e |
| AXOSOW01 | Pbca | 4.47 | 150 K | 2009 | 10.1107/S0108768109004066 |
| AXOSOW03 | Pbca | 4.47 | 150 K | 2015 | None |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes