# Amino pyrimidine Otolic acid cocrystal (Blind Test XV)

(Last updated March 2026)

Figure 1.  The molecular diagram of amino pyrimidine and otolic acid.

# CSP studies

| REFCODE | WICZUF |
| --- | --- |
| Formula | C13 H15 N3 O2 |
| Common Name | amino-pyrimidine otolic acid cocrystal |
| IUPAC Systematic Name | 4-methyl-pyrimidin-2-ylamine - 2-methylbenzoic acid cocrystal |
| Other Names |  |
| CSD Refcodes | WICZUF |
| Search Identifier | A |
| Scientist | Panos Karamertzanis |
| Date | 2008 |
| Publication | Day GM, 2009. Acta Crystallogr , Sect B 65, 107-125. |
| Energy model | 1 |
| Study_ID | 0 |
| Programs | MOLPAK, DMAREL (4.1.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\BlindTestXV\btxvcc_molpak |
| Potential Description | MP2 6-31G(d,p) DMA(1.1)+ fit.pots |
| Intramolecular Description | MP2 6-31G(d,p) |
| Search Identifier | B |
| Scientist | Panos Karamertzanis |
| Date | 2008 |
| Publication | Day GM, 2009. Acta Crystallogr , Sect B 65, 107-125. |
| Energy model | 1 |
| Study_ID | 10 |
| Programs | Flexible CrystalPredictor (1), Dmaflex, DMAREL (4.1.1) |
| Location on S Drive | \CHEMISTRY_CPOSS\0-EarlySearches\home\louise_price.eminerals\BlindTestXV\btxvcc_dmaflex |
| Potential Description | DMAflex GDMA2.1 + FIT |
| Intramolecular Description | MP2/6-31G(d,p) |

Figure 2.  Crystal energy landscape of amino pyrimidine and otolic acid from previous work.  Left: From MOLPAK (Energy Model A1).  Right: From CrystalPredictor and DMAflex (Energy Model B1).

# CSD structures (CSD version 6.01)

Table 1.  Crystallographic information for CSD entries for amino pyrimidine and otolic acid.  Different polymorphs are coloured differently.

| REFCODE | space group | Z’ | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° | density / g cm-3 | Form |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| WICZUF | P21/n | 1.0 | 7.27950 | 13.6699 | 12.6695 | 90.0 | 96.646 | 90.0 | 1.3009 | None |
| WICZUF01 | P21/n | 1.0 | 7.271 | 13.5961 | 12.6804 | 90.0 | 97.069 | 90.0 | 1.3095 | None |

Table 2.  Experimental information for CSD entries for amino pyrimidine and otolic acid.

| REFCODE | space group | R factor | T / K | Year | Comments |
| --- | --- | --- | --- | --- | --- |
| WICZUF | P21/n | 4.57 | 203 K | 2009 | 10.1107/S0108768109004066 |
| WICZUF01 | P21/n | 8.69 | 100 K | 2016 | None |

Make this table include whether polymorphs are solution-grown, sublimation grown, templated or otherwise.  Add references.

# Other notes